## Slide 1
ALD-deposited Multilayer to improve the superconducting performances of RF cavities
Yasmine Kalboussi1, Sarra Bira2, Baptiste Delatte1, Claire Antoine1, David Longuevergne2, Diana Dragoe3, Jocelyne Leroy4, Sandrine Tusseau-Nenez5, Aurélie Gentils2, Stéphanie Jublot Leclerc2, Fréderic Miserque7,Gael Sattonnay2, Enrico Cenni1, Mohamed Belhaj6, Thomas Proslier1.
1IRFU, CEA Saclay, 91191 Gif-sur-Yvette Cedex, France ; 2 Université Paris-Saclay, CNRS/IN2P3, IJCLab, 91405 Orsay, France ; 3 Plateforme ICMMO, Rue du doyen Georges Poitou, Bât 410 ,91400 Orsay France ; 4 Laboratoire d’Innovation en Chimie des Surfaces et Nanosciences, 91191 Gif sur Yvette, Cedex, France ; 5 Plateforme de Diffraction des Rayons X, Ecole Polytechnique, Route de Saclay, 91128 Palaiseau. 6 Physics instrumentation environnement space department, coupling of spacecraft and environnement unit, ONERA. 7 DEN, Service de la Corrosion et du Comportement des Matériaux dans leur Environnement (SCCME), CEA Saclay, 91191 Gif-sur-Yvette Cedex, France.

## Slide 2
Introduction
The multilayer is a stack of nanometric films of high Tc superconductors and insulators.
To synthesize this structure, we use atomic layer deposition ALD as a deposition technique as it well known to provide high quality Nano-films over large surfaces with complex shapes such as RF cavities.
[1] A.Gurevich,Enhancement of RF breakdown field of SC by multilayer coating.Appl. Phys.Lett, 2006.
| PAGE 1
An original approach proposed by A. Gurevich [1] to improve RF cavities through depositing a superconducting multilayer capable of screening efficiently the magnetic field.
To optimize this concept, we need as well a thermally stable diffusion barrier as a base and a low SEY material on the outer layer in order to limit multipacting inside the cavities.

## Slide 3: Ald Protective layer
RF test of the ALD-coated (Al2O3-10nm)cavity
First Step: Reduce Niobium native oxydes which are deleterious for superconductivity and replace it with a thermally stable ALD-deposited diffusion barrier.
Thickness profile on Si samples inside the Aluminium cavity
Gaz flow direction
  We manage to deposit uniformly a thin film of alumina.
  RF test shows a slight improvement of the Q0 at low field that increases with the accelerating gradient.
  Strong Multipacting barrier found at 18 MV/m that cannot be processed.
  Why and how to mitigate this effect?
Ald Protective layer
| PAGE 2

## Slide 4
Al2O3
SEY on ALD-deposited Films
| PAGE 3
Yasmine KALBOUSSI

## Slide 5
Al2O3
Bilayer AlN-NbTiN
| PAGE 4
Yasmine KALBOUSSI
Motivation: NbTiN has good superconducting performance (Tc = 17 K).
Chemistry: Combination of NbCl5/ NH3 and TiCl4/NH3 cycles:
n (TiCl4 + NH3) + m (NbCl5 +NH3)
NbTiN Chemical composition
Resistivity
Critical temperature
Ti content varies with TiCl4: NbCl5 Ratio non linearly.
Highest Tc by ALD without any post-treatment.

## Slide 6: AlN-NbTiN on cOpper 1,3 Ghz cavity
| PAGE 5
B
Before
After
AlN-NbTiN on cOpper 1,3 Ghz cavity
| PAGE 5
Yasmine KALBOUSSI

## Slide 7
Conclusion
| PAGE 6
  We manage to deposit uniformly a thin film of Alumina and reduce drastically niobium native oxides.
  RF test shows a slight improvement of the Q0 under low and medium Fields.
  TiN film is promising to reduce multipacting inside RF cavities.
  Growth of superconducting NbTiN by ALD with homogeneous composition and thickness control over large surface areas.
  Future Goals will be:
  Optimization of NbTiN process to improve superconducting properties.
  Test the NbTiN-AlN structure on Niobium RF cavities.
Thank you for your attention …