## Slide 1
ISMA’s development of detectors
for HEP experiments
II. Pulse shape discrimination
for particles identification
A. Boyarintsev, B.Grinyov, A. Kolesnikov,
T. Sibileva, P. Zhmurin
Institute for Scintillation Materials,
Kharkov, Ukraine

## Slide 2
ISMA’s development of detectors
for HEP experiments

## Slide 3
Motivation
New type of calorimeter - HGCAL
S1 (70-100Мrad) ~ 10% (inorganic scintillator or Silicon sensors)
S2 (5-70Мrad) ~ 65% (metamaterial scintillators)
S3 (up to 5Мrad) ~ 25% (plasticscintillators)
Actual task: cost-efficient detectors free of technological limitations
on overlapping large areas
S2
S3
S1
Scheme of radiation exposure zones
?
 | Silicon detector | Metamaterial scintillatiors
Radiation hardness | up to 100Mrad | up tо 100Мrad
Working temperature | - 30°С | + 25°С
Overlaping large area | yes | yes
Cost | high | Cost efficient

## Slide 4: Requirements for scintillation materials for high energy physics
  Physical and technical requirements
  Radiation hardness
  Short decay time
  Low activation
  Signal/noise ratio
  Ability to overlap large areas
“Shashlik” design
“Tile” design
Bulk scintillator
The transition from bulk scintillators to thin layers with alternation of absorber and scintillator
  Potential materials:
Al2О3
SiO2
Radiation-resistant components of the scintillation element are required:
- scintillator
- organic optical medium
- light guide

## Slide 5: Scintillation crystal selection
 | Activator concentration | Decay time, ns | Light yield, ph/MeV | Emission λmax, nm
LYSO:Ce | 0.2% | 41 | 30000 | 397
YSO:Ce | 0.1% | 70 | 30000 | 420
GSO:Ce | 0.5% | 60 | 12500 | 430
GPS:Ce | 7.0% | 46 | 30000 | 372
YAG:Ce | 0.1% | 100 | 15000 | 550
GGAG:Ce | 0.2% | 50 | 50000 | 530
YAGG:Ce | 0.1% | 15 | 15000 | 500
Al2O3:Ti | 0.1% | 3400 | 18000 | 750
Silicates -LYSO:Ce (Lu1.8Y0.2SiO5:Ce) -YSO:Ce (Y2SiO5:Ce) -GSO:Ce (Gd2SiO5:Ce) -GPS:Ce (Gd2Si2O7:Ce) | Garnets -YAG:Ce (Y3Al5O12:Ce) -GGAG:Ce (Gd3Al2.5Ga2.5O12:Ce) -YAG:pure -YAGG:Ce (Y3AlGa4O12:Ce) | Saphire - Al2O3:Ti

## Slide 6: Radiation hard scintillation element
after irradiation
Essential overlapping
of YSO:Ce emission spectrum and YAG:Ce (or YAGG:Ce) absorption spectrum
Decay time YAGG:Ce, Ca fiber before and after irradiation with dose of 50 MRad
before irradiation

## Slide 7
Radiation hardness of polysiloxanes
Irradiation with electrons (E0 = 8.3 MeV) up to 300 MRad dose
ISMA (Kharkov) tests
Haiying Xiao et al., Journal of Applied Polymer Science, ·2008
Plates made from SKTN (D) polymer resins (a) and Bicron-600 (b).
Irradiated by neutron with fluency 0 (#0), 16*1014 (#1), 3.8*1014 (#2) and 1.2*1014 сm-2 (#3).
Irradiation with neutrons (E > 1 MeV)
JINR (Dubna) tests
a
b
Irradiation with protons (150 KeV)
Space Materials and Environment Engineering Laboratory, Harbin Institute of Technology (Harbin) tests
The tests were carried out in several scientific institutes of the world

## Slide 8
Two main types of Pt-cured Polysiloxanes
Polymethyl siloxane
Polyphenyl siloxane
Polysiloxane
- High strength Si–O bonds preserves transparency of polysiloxane up to high irradiation dose;
- Mechanical hardness is increased by the presence of phenyl groups absorbing part of radiation energy due to π-electrons in aromatic rings
Radiation hardness of Polysiloxanes vs. Scintillation plastic
Plastic scintillator
- Decrease in transparency because of the destruction of C–H and C–C bonds, production of free radicals and C=C bonds as absorbing centers

## Slide 9
Polysiloxane-based scintillators for “shashlyk” calorimeters
F. Acerbi et al., Nuclear Inst. and Methods in Physics Research, A 956 (2020)
The calorimeter provides particle identification capabilities and energy resolution for electrons
at the same level as for standard plastic scintillators
Margaret Bowen et al., IEEE Transactions on Nuclear Science, 1989
no yellowing with doses up to 100 kGy
light outputs ranging from less than 5% to 90%
of a reference sample (BC-408)

## Slide 10: Polysiloxane based scintillator
DIPHENYLSILOXANE
POLYPHENYLMETHYLSILOXANE
# | L0 (L) | L/L0, % | D1/2, МRad
3 | 3666 (2090) | 57% | 12,3
4 | 3821 (3029) | 79% | 29,8
# | L0 (L) | L/L0, % | D1/2, МRad
1 | 2364 (1500) | 63,5% | 15,2
2 | 4228 (2450) | 58% | 12,7

## Slide 11
Radiation damage of polysiloxane based scintillator
Radiation damage:
fluorescent dyes
polymer network
Under ion beam irradiation the light emission of polymers decreases
The radiation hardness more than 20 MRad was reached due to the new activators
 | 1214 | 1280 | 1278 | 1272 | 1301 | 1309
D1/2 | 7,6 | 15,7 | 14,3 | 14,5 | 20,6 | 21,2

## Slide 12
3D printing technology for metamaterial detectors
FDM 3d-printer
Filament Extruder
Optically clear pellets
Scintillation filament
Inorganic scintillation powder
+
The modes for obtaining of filaments doped with inorganic powders have been determined
1
2
3
4
As scintillation powders were used ZnSe:Al, GOS:Pr, GaGG:Ce and CsI:Tl with weight content from 30 to 75%

## Slide 13
3D printing scintillator technology
Thin layer scintillation films with spatial resolution up to 3.35 lp/mm were obtained
Scintillation filaments with a weight content of inorganic powders up to 75% were obtained
Plastic scintillator with reflector
Results obtained are in good correlation with the data for industrial samples
1
2
3
4
5
6
Scintillators for registration of alpha- and beta-particles and gamma-photons
3D-printing technology has ample opportunities in the creation of scintillation detectors

## Slide 14
II. Pulse shape discrimination for particles identification

## Slide 15
Classical spectrometer (scintillation pulse area analysis)
Scintillator
Photo detector
PreAmp
50 us
Shaper
MCA
Scintillator
Photo detector
PreAmp
Fast
ADC
FPGA
Soft 1
Digitizer
PC
Soft 2
Digital spectrometer for pulse shape analysis
All events
True shape pulses

## Slide 16
Comparison of classical and PSD spectrometry
 | Advantages | Drawback
Classic MCA | -Cost-efficient -Standard PHR -Optimal technical resource | -PSD impossible
Pulse shape discrimination analyses | -The events discrimination by pulse shape -Analysis of pulse shape -Improve PHR | -Overlarge data file , preliminary filtering of data is required
Causes of pulse distortion
Normal pulse
Superposition
of two pulses
Noise as an pulse
Selection of a pulse with an amplitude close to noise

## Slide 17: Pulse shape discrimination methods for neutron\gamma separation
Image PSD
FOM = Qslow / Q total
PSD by image (soft2)
Scint.
Photo
detector
Pre Amp
Fast
ADC
FPGA
Soft 1
Digitizer
Classic PSD method

## Slide 18
Neutron/gamma discrimination
Conventional
PSD by image
Theory
In practice
The separation N/G low amplitude pulse it is a general task
Low amplitude pulse
High amplitude pulse
Noise under the signal

## Slide 19
Аlpha/beta discrimination
Conventional
Alfa/betta separation by energy
PSD image
The material selection with a specific pulse form
Alfa/betta discrimination by pulse form due slow and fast scintillators (plastic and ZnS(Ag)
Alfa/betta PSD

## Slide 20
NaI – excellent spectrometry
Large area NaI + Plastic scintillator
PS + NaI – high sensitivity and spectrometry available
- increased sensitivity to registration of back scattering gamma quantum
- image spectrometry
PS – excellent sensitivity for energy high than 300 keV
Fig. 1. 50x250x1000 mm3 gamma detector
1 – Plastic scintillator
2 – NaI(Tl) or CsI(Tl) layer
3 – Reflector
4 – Housing
5 - PMT
1 – Plastic scintillator
2 – NaI(Tl) or CsI(Tl) layer
3 – Reflector
4 – Housing
5 - PMT
Spectrometry for multimaterial detectors

## Slide 21
Spectrometry for multimaterial detectors
We applied PSD for separation of “suitable for spectrometry” signals and filtered “impeding” signals from PS (it is actual for complex spectrum)
NaI pulses are suitable for spectrum creation and isotopes identification
PS pulses don’t provide information about peaks and aren’t used in spectrums
PS pulses
NaI + PS pulses
NaI pulses
(NaI + PS) pulses describes backscatter peaks

## Slide 22
“Improved” spectrometry
4 peaks are resolved.
Peak 2614 keV isn’t resolved because of the small thickness of NaI(Tl).
Statistical methods are required “improved” spectrometry with PSD

## Slide 23
Thank you for your attention!